:

Page 1:   Table of Contents

Page 2:   Background and Fig. 1

Page 3:   Origins and Fig's. 2, 3, 4

Page 4:   Magneto Slipper Flywheel

The Lanchester Patent

Royce's First Damper Patent

Fig's. 5, 6

Page 5:   Friction Material and Fig. 7

The "Eagle" and Aero

Page 6:   Fig's. 8, 9, 10

Page 7:   Further Auto Damper Developments

Current Status and Fig's. 11, 12

Page 8:   Fig's. 13A, 13B

Page 9:   Damper Performance

Royce Damper Modeling

The Importance of Cylinders

Page 10:  Fig's. 14, 15

Page 11:  Fig's. 16, 17

Page 12:  The Final Royce Damper

"Sticking" Dampers and Tufnol

Page 13:  Fig. 18A and the Merlin

Page 14:  Fig. 18B and the Magic of Merlin

Page 15:  About the Author

Page 16:  Material Analysis Addendum #1

Page 17:  cont'd

Page 18:  Material Analysis Addendum #2

Page 19:  cont'd

Page 16 (addendum #1- John Crofts)

COMPARISON OF FRICTION MATERIALS IN R-R DAMPER.

Further to the data in "Hose Clamp, Technical Supplement Vol 27-TI,

1998", concerning suitable friction material for substitution in Rolls-Royce and Bentley crankshaft friction dampers, more details are offered:

1 . A test rig was set up to simulate certain operating conditions in a typical friction damper (early Mk VI type), to compare a range of alternative friction disc materials in regard to torque at break-away and under running conditions; the effect of lubricant types; and the loading pressure required to produce a constant level of running torque.

* A 14" x 40" center lathe was used, with the rear floating inertia member (see Fig. 11 of reference paper) mounted in the lathe chuck, and the center member (normally keyed to the crankshaft), forced against the friction disc on test by the tailstock while restrained from rotating by a torque wrench of the bending beam type, resting against a support. This was used because it is a simple device, providing consistent results from test to test, and is very sensitive to vibration from the "slip-stick" behavior of certain materials.

* Between the tailstock and the torque wrench head a small hydraulic cylinder was centered, with a pressure gage attached, calibrated from 0 - 1500 p.s.i. This indicated the force required to produce a consistent torque level between the rotating and fixed elements.

* Three types of oil were used for comparison purposes, a) a light hydraulic oil; b) a commonly used automotive engine oil of 5W-30 SAE grade, with an API duty rating of SJ/SH, and c) a gasoline/diesel engine oil of SAE 15W-40 grade, with an API duty rating of CG4/SH with extended life additives.

2.	The friction materials used were 1) original R-R cotton disc, used but in

excellent condition. 2) Smooth plastic material (Acco). 3) Soft cardboard. 4) Heavy

grade	cartridge paper). 5) Aluminum sheet. 6) Raybestos clutch lining. 7) HO 21

material. 8) HO 101 material. 9) HO 121 material. 10) Tufnol replacement disc for

a P.11.	11) Tufnol replacement disc for a 31/2 Liter Derby Bentley.

(No's 7; 8; & 9 were supplied by Hoerbiger GMBH, and are commercial heavy

duty friction materials. No's 10 & 11 are thought to be "Tufnol", a smooth plastic

laminated with fabric', from independent R-R/B parts suppliers).

* The procedure followed was to clean up the two metal surfaces of the old Mk VI damper by polishing with an angle grinder using fine emery discs. No machining was used, as the original surfaces were flat, but marked with rust grooves from the original cotton radial strands. These were mostly polished out, but slight witness marks were left, as representing a reasonable job of "cleaning up" the components by an owner lacking machine shop facilities.

continued:

Page 17 (addendum #1 cont’d – John Crofts)

* The friction material was liberally coated on both sides with fresh lubricant, and the system run at 60 rpm (the lowest speed of the lathe headstock) for several minutes until a temperature of about 120 F on the stationary pressure plate was attained. Data logging then began, with cleaned plates and fresh lubricant applied for each new material sample. This procedure maintained the metal temperature with a preliminary run of 1 minute for each sample.

* A rotating torque setting of 20 lb.ft. was maintained by adjusting the force applied by the tailstock, and after one minute of running the rotation was stopped, and the chuck barred over with a tommy bar to read the break-away torque value. The rig was again set in motion to ascertain that the running torque level had not changed.

3. Results:

The objective was to match as closely as possible the performance of the original R-R Cotton, material 1).

* Five of the materials tested were disqualified by reason of vibration while running, and/or requiring excessive force (beyond the capacity of the pressure gage) to obtain the standard test torque of 20 lb.ft. These were No's: 2) Smooth plastic; 3) Soft cardboard; 4) Cartridge paper; 5) Aluminum sheet-, and 6) Raybestos clutch lining material.

* The most consistent results (many repeat tests were conducted), were obtained with the gasoline/diesel engine oil of SAE grade 15W-40. This is most likely due to the additive package in this lubricant, and also confirms Hoerbigers comment that the nature of the oil does affect the results obtained.

* The remaining material performances are tabulated below:

Material    Breaking torque     Running torque	     Torque Ratio             Pressure*

1) Cotton	18 lb.ft.	20 lb.ft.	1.11	10.24 p.s.i.

Very smooth break-away

7) HO 21	18 lb.ft.	20 lb.ft.	1.11	15.33 p.s.i.

Very smooth break-away

8) HO 101	19 lb.ft.	20 lb.ft.	1.05	14.75 p.s.i.

Smooth break-away

9) HO 121	19 lb.ft.	20 lb.ft.	1.05	13.59 p.s.i.

Less smooth break-away, occasional very slight vibration.

10) P.11 Tuf.	27 lb.ft.	8 lb.ft.	0.29	15.90 p.s.i.

Harsh break-away, smooth when running.

11) D.B.Tuf.	22 lb.ft.	10 lb.ft.	0.45	19.75 p.s.i.

Harsh break-away, smooth when running.

*Note: The pressure listed is the unit pressure per square inch of the friction

material discs, 1-9 = 6.5" x 4.5"; 10 = 6.38" x 4.13"; 11 = 5.88" x 4.0".

Material thickness = 1,10, 11) 0.062"; 7) 0.050"; 8) 0.048"; 9) 0.030".

The Hoerbiger materials can be obtained in several thicknesses.

Page 18 (Addendum #2 – John Crofts)

VIBRATION DAMPER MATERIAL ANALYSIS

Summary:

This is the second addendum to the paper "Rolls-Royce & Torsional Vibrations", Volume 27-Tl of "Hose Clamp", the news letter of the Pacific North-West Region, RROC, published in 1998.

It complements the first addendum, which was a listing of the physical performance attributes of a series of friction materials, with the purpose of ranking them against the original cotton duck material supplied by Rolls-Royce for many years for their friction crankshaft dampers used on 6-cylinder car engines from 1912 to 1956. Two additional materials have been tested in the same manner as the first batch of 10 alternative materials, compared to an original R-R cotton duck disc.

Comparisons:

The two additional materials are compared to the original and the two best alternatives previously tested, using the same test rig, a 14 center lathe, and the same damper components, with the most consistent lubricant found on the first series of tests, Shell Rotella'T' 15W-40 SAE grade.'

Material             Breaking Torque	Running Torque                  Torque Ratio                Pressure

1) Cotton                18 lb.ft.	    20 lb.ft.                                1.11                          10.24 p.s.i.

Very smooth break-away

7) HO 21                18 lb.ft.	    20 lb.ft.                                1.11                          15.33 p.s.i.

Very smooth break-away

8) HO 101              19 lb.ft.                 20 lb.ft.                                1.05                          14.75 p.s.i.

Smooth break-away

12) Fiennes            18 lb.ft.                 20 lb.ft.                                 1.11                          17.10 p.s.i.

Very smooth break-away

13) Ferodo             24 lb.ft.                 20 lb.ft.                                 0.83                          19.2 p.s.i.

Violent vibrations under all conditions.

The sample 12) was furnished by Fiennes Engineering of Clanfield Mill, G.B., and gave a very similar performance to the two best samples, the original cotton, and H021 material from Hoerbiger.

The difference between these two alterative materials is insignificant performance-wise, but it would help to understand the behavior of the material at high temperatures. The H021 material is specifically developed for use in spring dampers for lock-up clutches in automatic transmissions, and has a very high temperature & wear resistance, consistent with this type of usage.

(continued)

Page 19 (Addendum #2 – John Crofts)

The porous Polypropylene material from Fiennes may not have been bench-tested for high-temperature wear, or friction co-efficient stability characteristics, bearing in mind that it needs to be able to operate successfully, with a long life, under the following conditions-

Between steel rubbing surfaces of 200 to 250F, with an additional heat input rate of 2.5 watts1square inch of friction material, when running at 4, 000 engine rpm. These are the conditions in an engine at high speed during summer.

The Ferodo material was taken from an R-R servo lining replacement, based on information from James Pate of the RROC, who has anecdotal . information from members of the RREC, about the mysterious Modification note contained in Bulletin BB.234, for the Z series of 6-cylinder cars produced at Crewe.

These were the last of the 6-cylinder engines produced by Rolls-Royce, and the note says "Ferodo washers and drain slots in the crankshaft vibration damper", from chassis B-212-ZY onwards.

There is conflicting information regarding this modification, as Hermann Albers of Albers, Rolls-Royce in Zionsville, IN, told the writer that he had a sample of a cotton duck washer with the word 'Ferodo' clearly stamped on it. However the anecdotal information states that the material first used for this modification was the same material as is used for the servo linings, and the slots were cut in the friction face of the material to allow of oil ingress across the face, as the material is not highly absorbent like the cotton, and would tend to wipe dry without the oil slots.

The test of this material was done using a servo liner, which has rivet holes around the face, thus allowing oil to be distributed across the working area, but the vibratory characteristics were very severe, smooth running could only be obtained by very gentle application of load, and severe vibration was immediately precipitated by any load above about 10 lb.ft. running torque, and also when testing break-away torque. The loading required to reach an acceptable torque was also higher than the other satisfactory materials tested, and would probably have required spring modifications in the damper.

It may be that the original Ferodo material was found to be unsatisfactory in service or production. and was replaced by Ferodo by a more suitable material?

Page 20 (Addendum #3 – John Crofts)

ROYCE SLIPPER DAMPER MATERIAL TESTS:

This is the 3rd addendum to “R-R & Torsional Vibrations”, Vol. 27-T1 of the Hose Clamp magazine.

Two additional friction materials have been tested in an effort to give R-R owners and repairers a satisfactory substitute with known properties, for the original R-R cotton discs.

The two new materials were tested in the same way as the previous units, including the original R-R cotton disc, which is listed for comparison.

Material	Breaking Torque	Running Torque	Torque Ratio	  Pressure

R-R Cotton	18 lb.ft.		20 lb.ft.		1.11		  10.24 p.s.i.

Very smooth break-away

14) N-411	18 lb.ft.		20 lb.ft.		1.11		   12.29 p.s.i.

Very smooth break-away

15) JDDW	27 lb.ft.		20 lb.ft.		0.74		   13.93 p.s.i.

8385	Smooth break away, very slight vibration when running.

Both materials were supplied by S.K.Wellman Co. of Canada, address:

606, Rivermere Road, Unit 10,

Concord,  ON  L4K2H6

Canada.   Contact: Mr. Paul Douglas, Tel: 905-669-1301  Fax: 905-669-4124

The N-411 material is smooth, dark, porous material, normally used as a friction braking disk for heavy-duty truck clutch brakes. This is a very rugged application with marginal, if any lubrication. This material is close to the R-R cotton in all respects, requiring perhaps slightly higher spring pressure.   It is marked “Texon” and is 1/16” thick, the same as the original cotton.

The JDDW 8385 is a woven and bonded material used for emergency brakes required by law in Europe on farm tractors when used on public highways. This material is not suitable as a replacement due to the lower torque ratio, the higher pressure requirements and the more aggressive action.

A heavy-duty gasoline/diesel engine lubricant meeting SAE CF/SJ requirements, of 15W-40 grade, (Valvoline Premium Blue 2000), was used for this test, (which is a desirable lubricant for classic R-R/Bentley engines), and the friction discs were soaked in the oil for two hours @ 45F before the test, to assure representative performance. Metal temperature during the testing was approx. 125F.

John G. Crofts

Principal engineer